Adsorption-based technologies for innovative, sustainable & onsite hydrocarbon remediation

# Context and challenge

Most of existing processes operated by the oil industry to separate hydrocarbons (HC) from water or sand are gravimetric, either under simple forms (such as settling tanks) or enhanced by some means such as centrifugation (cyclones) or temperature increase. The particle sizes are often the limiting factor, but also the apparent density of the HC, which can be greater than the density of water, mainly when the HC are mixed with contaminants such as sand/inorganic particles.

In the case of the oil sand industry, large amounts of heated water permit the reduction of the HC viscosity which facilitates the separation of the HC from their contaminants (mainly inorganic matters: sand and clay).

The HC extraction process developed by OHT (later called “the OHT process”) is not based upon gravimetry, but upon surface chemistry. The efficiency of the HC extraction is linked to the probability of contact between an oleophilic agent and the HC. After the extraction phase, the HC rich agent is separated from the depolluted environment and either treated for the recovery of the HC or used for the production of heat /energy.

An extensive test program has proven the OHT process efficiency on all types of HC studied and therefore this process can be envisaged virtually in all the situations where HC have to be removed from their environment. It also confirms that the OHT process operates at ambient temperatures and needs limited quantities of water.

OHT has been demonstrated on sites at pilot level. A pilot for produced water treatment was tested in Germany for 3 months with success.

# The OHT process

The novel and innovative process developed by OHT to extract the Hydrocarbons (HC) from their environment combines:

- A polymeric adsorption agent (later called “the agent”), which is both oleophilic and hydrophobic, and which can selectively adsorb and release HC during the process. This reversibility confers to the agent the capacity to be reused several times in a cyclic process.

- The agent is fabricated to combine the efficiency of HC adsorption and desorption as well as a mechanical strength permitting its reuse in successive cycles (100 times).

- A HC extraction/production process which makes use of the agent and aims at efficiently extracting and eventually restituting the HC contained in the water or soil.

The OHT process includes 3 main steps:

- The extraction step, during which the agent comes into contact with the HC-containing matrix (polluted soil or water, produced water). Then the HC is selectively extracted from this matrix.

- The agent separation step, during which the HC-rich agent is separated from the matrix.

- The desorption step, during which the oil-rich agent is treated in order to recover the oil.

It must be emphasized that the OHT process has two innovative characteristics:

- In the OHT process, which is not based on a gravimetric principle, water is not the vector of the HC separation.

- The OHT process does not require large quantities of energy and can be carried out at ambient temperature.

# Adaptability of the OHT process to various applications

In order to study the versatility of the OHT process, several tests have been performed on a large range of samples, from produced water to oil sands and lightly polluted soils. In this paper we will focus on the last results of produced water treatment at pilot level.

Tests carried out at laboratory scale yielded very positive results (~100% HC extraction). As the OHT process appears to be efficient on a wide range of HC and at low HC concentrations, its adaptation to the treatment of the water produced by the petroleum industry (produced water) has been identified as a potential application. A specific project was developed in collaboration with industrial partners from 2012 to 2014.

This pilot unit, which had a treatment capacity of ~10 m3/h, included two variations of process implementation: a dynamic process and a static process.

Process advantages

- Simplifies of the overall process water management,

- Reduces in the global duration of treatment,

- Saves space (relevant for offshore platform and FPSO applications),

- Increases treatment efficiency, providing increased production and compliance with the more stringent discharge regulations (dissolved hydrocarbons, PAHs ...)

- Decreases CAPEX, OPEX (no chemical additives) and maintenance costs.

Test parameters:

- HC content of inlet PW: between 150 and 700 mg/l

- PW flowrate: between 2 and 10 m3/h

Figure 1 : HC concentration before and after treatment by OHT process

Main results of this pilot-level test are as follows:

- HC extraction yields averaging 98% were achieved;

- Recovery of HC from the oil-rich agent was achieved without solvent addition, we use a centrifugation;

- Extraction efficient is not influenced by flowrate or HC concentration.